HT-5299 two-part silicone compound

●INTRODUCTION

·HT5299 is a addition 2-part and flame retardant silicone compound.It is suitable for potting dense electronic component packages requiring heat dissipation as it has low viscosity and high thermal conductivity. This compound has excellent thermal stability, electrical properties, is compatible with most electrical insulating  materials and has a UL 94 Flame Rating of 94 V-0.

●APPLICATIONS

·General potting applications: power supplies,

connectors, sensors, industrial controls,

transformers, amplifiers, high voltage resistor

packs, relays

●HOW TO USE

·Before mixing, part A and part B should be

stirred adequately in container.

·Supplied as two-part liquid component kits

comprised of Part A/Part B to be mixed in a

1:1 ratio by weight or volume; automated

mixing and dispensing; manual mixing.

·After mixing,it can be heated to accelerate the cure rating.

●NOTICE

It can not cure if contact with three substance therein after:

·N, S, P organic compound

·Sn、Pb、Hg、As ionic compound.

·Alkyne and ethylene compound.

●TYPICAL PROPERTIES

| As Supplied（25℃，65％RH） |  |  |
| --- | --- | --- |
| Part | 5299 A | 5299 B |
| Color，visual | Gray | White |
| Viscosity，cps | 5500 | 3500 |
| Specific Gravity | 1.58 | 1.58 |
| Properties after mixing（25℃，65％RH） |  |  |
| Mixing Ratio(by weight) |  | A：B = 1：1 |
| Color |  | Gray |
| Mixture viscosity，cp |  | 4000 |
| Pot life，min |  | 30 |
| Curing time，，h |  | 24 |
| Curing time 80℃，min |  | 30 |
| Cured，25℃，65％RH |  |  |
| Durometer Hardness, Shore A |  | 65 |
| Tensile strength，Mpa |  | 3.5 |
| Elongation at break，% |  | 50 |
| Coefficient of thermal expansion,℃ |  | ≤2.2×10-4 |
| Thermal Conductivity，W/m.K |  | ≥0.60 |
| Electrical |  |  |
| Volume resistivity ，Ω·cm |  | ≥1.0×1014 |
| Dielectric strength， kV/mm |  | ≥22 |
| Dielectric constant at 1.2MHz |  | 2.9 |
| Dissipation factor at 1.2MHz |  | 0.005 |

●PACKAGING AND SHELF-LIFE

·PACKAGING： A：10kg;  B：10kg

·SHELF-LIFE：12 months